## Slide 1: An Introduction to Fe-based superconductors
Yuen Yiu
University of Tennessee, Department of Physics and Astronomy
Knoxville, TN 37922

## Slide 2: Overview
Brief history: Discovery and progress
Material variations: 4 types of material: “1111”, “122”, “111” and “11” [10]
Experiments and physical properties:
Transport properties, magnetic properties, crystal structures, phase diagram
Theoretical models

## Slide 3: Brief History
Reported by Kamihara et al. on 19rd March 2008, paper titled
“Iron based superconductor La[O1-xFx]FeAsO with Tc=26K” [12]
has been cited for 1,117 times as of 4th March 2010!
Only non-cuprate high Tc superconductors (Tc>20K)
Very popular at the moment: There is at least one presentation session EVERY DAY at the upcoming APS March meeting
Table 1 Maximum Tc in each RFeAs(O1-xFx). The F concentration x, which gives the maximum Tc is shown [10]

## Slide 4: Material variations
“1111” family
“122” family
RFeAsO
(R can be but not limited to: Ce, Pr, Nd, Sm, La)
Superconductivity induced by Oxygen site electron doping (usually with F), or simply creating oxygen deficiency
Iron site electron doping has also been reported
AFe2As2
(A = Ba, Sr, Ca, etc.)
SC induced by A-site doping with monovalent B+ (i.e. K, Cs, Na, etc.)
Iron site doping with Co has been reported

## Slide 5: Material variations
“111” family (?)
“11” family
Li-deficient LiFeAs superconducts
Superconductivity very sensitive to sample preparation [10]
Parent compounds superconducts (?)
Not as popular
Simplest structure
Se-deficient FeSe superconducts up to 8K [10]
NOTE: the PARENT COMPOUNDS DO NOT SUPERCONDUCT UNDER AMBIENT PRESSURE!!!

## Slide 6: Crystal structure
“1111”: layers of FeAs and LaO
“122”: layers of FeAs and K/Sr
“111”: layers of FeAs and Li
“11”: layers of FeSe
Figure 1
(a) Crystal structure of LaOFeAs; [2]
(b) Crystal structure of (K/Sr)Fe2As2 and (Cs/Sr)Fe2As2 [2]

## Slide 7: Sample Synthesis
EXAMPLE:
Polycrystals: conventional solid state reaction.
PrFeAsO: start with PrAs, Fe2O3 and Fe powders. Ground up stoichiometric mixtures in glovebox, pressed into pellets, sealed in silica tubes in argon, and then heated at 1200oC for 30 hrs. [11]
Figure 2 A picture of what PrFeAsO powder looks like

## Slide 8: Transport properties
Figure 3 Temperature dependence of electrical resistivity of LaFeAsO1-xFx. The inset is a phase diagram constructed with the data. [9]
Broad peak at T~150K is generally associated with the SDW phase transition
The transition is suppressed and shifted to a lower temperature as doping level increases
Superconductivity emerges at x=0.03

## Slide 9: Neutron Powder Diffraction
Figure 4, 5, 6 (left) NPD data for PrFeAsO [5]; (center) Lattice parameter v. Temperature data showing structural transition [Yiu Y. et al., unpublished]; (right) Lattice parameters v. doping level [8]
Peak splitting: tetragonal-orthorhombic structural transition
(Extra) Magnetic peaks found at 5K

## Slide 10: Behold! The General “1111” Phase Diagram
Figure 7 The structural, magnetic, and superconducting phase diagram of PrFeAsO1−xFx [3]
Suppress the following and SC will EMERGE! Structural transition, magnetic phase transition (Naïve, experimentalist point of view)
Can be done by chemical doping or applied pressure

## Slide 11: Behold! The General “122” Phase Diagram
Figure 8 The structural, magnetic, and superconducting phase diagram of BaFe2-xCoxAs2 a member from the122 family [14]
Superconductivity coexists with antiferromagnetism!??
Interesting…

## Slide 12: Theoretical models
Non BCS theory of superconductivity!?
Works suggesting the s±-pairing state
Unconventional and mediated by (nesting-related) antiferromagnetic spin fluctuations [13]
First example of multigap superconductivity with a discontinuous sign change between the bands [13]
Similar but different from the famous superconducting MgB2 [13]
No common consensus yet

## Slide 13: Conclusions
“Fe-based superconductors” is a new and exciting field
4 different types of crystal structure found in this group
The parent compounds do not superconduct, but undergo a structural distortion, a SDW phase transition and magnetic ordering instead.
These transitions can be suppressed by chemical doping or applied pressure (unexplored today) and superconductivity will emerge
No universally accepted theoretical model yet

## Slide 14: References
[1] Liu R. H. et al, Phy. Review Letters, 101, 087001 (2008)
[2] Sasmal K. et al, Phy. Review Letters, 101, 107007 (2008)
[3] Rotundu C. R. et al, Phy. Review B, 80, 144517 (2009)
[4] Ren Z. A, Materials Research Innovations 12, 1 (2008)
[5] Zhao J. et al, Phy. Review B, 78, 132504 (2008)
[6] Qi Y. P. et al, Phy. Review B, 80, 054502 (2009)
[7] Wang et al, Phy, Review B, 78, 054521 (2009)
[8] Han F. et al, Phy, Review B, 80 024506 (2009)
[9] Dong J. et al, Europhys. Letter, 83, 27006 (2008)
[10] Ishida k. et al, Journal of the Phy. Socity of Japan, 78, 062001 (2009)
[11] McGuire M. A. et al, Journal of Solid State Chemistry, 182, 8, p 2326-2331 (2009)
[12] Kamihara et al., Journal of American Chemical Society, 130, 11, p. 3296+ (2008)
[13] Mazin I. I. et al., Phys. Rev. Lett., 101 057003 (2008)
[14] Wang X. F. et al., arXiv:0811.2920.